## Slide 1: SAND AND SILICA SAND
SILICA (Si) is the 2nd most abundant element on earth’s crust
Commonly found in its oxidized form as Silicon Dioxide (SiO2)
Sand is a naturally occurring granular material comprised of finely divided rock and mineral particles
Sand is transported by wind & water and deposited in the forms of sand beaches, dunes, sand splits, sand bars ( placer deposits) etc.
Sands, largely constituted of silica, in the forms of quartz, and iron oxides
Heavy Mineral Sands (Black Sands):
  Zircon, ilmenite, monazite, rutile, xenotime, struverite and garnet etc are co- or by-products for heavy mineral sands
  These are the important sources for zirconium, titanium. thorium, tantalum and other rare earth elements
Washed Sand
Silica Sand
Heavy Mineral Black Sand

## Slide 2: Product Categorization & Code
Product Name | Product Family Code | Specifications |  |  |  |  |  | Final Product Code
 |  | Silica Content (Si %) | Iron Content ( Fe%) | Calcium Content (Ca%) | Titanium Content (Ti%) | Size |  | 
 |  |  |  |  |  | mm | Mesh (US) | 
Kim-Sil (KS) | 960 | 96.00 | 0.08 | 0.9 |  | 0.5 – 2.38 | 35 - 8 | KS 960-08
Kim-Sil (KS) | 985 | 98.50 | 0.05 |  |  | 3.36 – 10.0 | 6 – 0.394 inch | KS 985-05
Great Fuma (GF) | 990 | 99.0 | 0.05 |  | 0.05 | 0.105 – 0.841 | 140 – 20 | GF 990-05
Great Fuma (GF) | 992 | 99.20 | 0.03 |  | 0.05 | 0.105 – 0.595 | 140 -30 | GF 992-03
Great Fuma (GF) | 995 | 99.50 | 0.02 |  | 0.03 | 0.105 – 0.595 | 140 -30 | GF 995-02
Product Name Family Code-Iron %
KS 960-08

## Slide 3: Silica Sand Washing Plant

## Slide 4: Silica sand stockyard and loading to vessel
SILICA SAND STOCKYARD
SILICA SAND LOADING AT LUMUT PORT

## Slide 5: Enhanced Silica Production Flowchart

## Slide 6: Silica WASHING PLANT
Washing Plant with the capacity of 400mtph

## Slide 7: Quality System for silica production
Quality Inspection focuses:
Incoming inspection for raw sand (Fe, Si, Ca, etc)
In-process inspection for grain-sizes (125-800µm)
Final quality inspection for outgoing (Fe, Si, Ca, Ti, Al etc)
Pre-shipment inspection for shipment (Fe, Si, Ca, Ti, Al, grain-size, etc)

## Slide 8: Silica sand for glass and chemical applications
S/No | Characteristic (% by Mass) | Requirement |  |  |  | 
 |  | Special Grade 1 | Special Grade 2 | Grade 1 | Grade 2 | Grade 3
1 | Loss on Ignition, Max | 0.5 | 0.5 | 0.5 | 0.5 | 0.5
2 | Silica (as SiO2), Min | 99.5 | 99.2 | 99.0 | 98.5 | 96.0
3 | Iron Oxide (as Fe2O3), Max | 0.02 | 0.03 | 0.05 | 0.05 | 0.08
4 | Aluminium Oxide (as Al2O3), Max | 0.025 | 0.035 | 0.035 | 0.05 | 0.05
5 | Titanium Dioxide (as TiO2), Max | 0.015 | 0.015 | 0.03 | 0.03 | 0.03
6 | Manganese Oxide 9asMnO) | 0.015 | 0.015 | 0.03 | 0.03 | 0.03
7 | Copper Oxide (as CuO) | 0.015 | 0.015 | 0.03 | 0.03 | 0.03
8 | Chronium Trioxide (as Cr2O3) | 0.015 | 0.015 | 0.03 | 0.03 | 0.03